| *AUTOMATIC SINTERING MACHINE mod. 10STV, WITH CONTROLLED ATMOSPHERE, 1 STATION 60Kva MONOPHASE, 26TON. |  |
| --- | --- |
| Main Features |  |
|  Sintering machine suitable for producing segments and small series of diamond tools. |  |
|  Mould heating system for direct passing of alternate current.(Joule effect) |  |
|  Sintering with graphite moulds. |  |
|  Sintering under controlled atmosphere by means of vacuum/inert gas programmable wash. |  |
|  K – type thermo-couples for operating temperatures of up to 1000°c. |  |
|  Cooling plates, transformer and vacuum chamber with flow visualisation and water temperature. |  |
|  60 kVA Monophase transformer, (maximum power is limited electronically to 165A) by switch for 5 different tensions between the electrodes (maximum power limit for heating). |  |
|  Controller program with cycles divisible into 12 steps. Each step includes: |  |
|  temperature |  |
|  pressure |  |
|  max. power limit |  |
|  heating time |  |
|  holding time |  |
|  Compression force controlled electronically (loop system) |  |
|  Process data visualisation (set and real) and alarms. |  |
|  Machine complies with EEC regulations. |  |
| Options |  |
|  Temperature control by means of optical pyrometer 350 – 1300°C. |  |
|  Segment height control while sintering takes place (linear transducer on cylinder, resolution of 0,01mm) |  |
|  Data acquisition system on external PC. |  |
|  Regenerative system for the reduction of minimum compression force (from 1700 to 700kg). |  |
|  Electrodes in graphite and amorphous carbon. |  |
|  Aluminium frames. |  |
|  Graphite plates. |  |
|  Graphite moulds. |  |
|  Prearrangement for modem installation for remote assistance. |  |
| Technical data |  |
|  Max. sintering area | 60 cm2 (850°C; 350kg/cm2) |
|  Power supply | 380 / 400V 3phs 50Hz |
|  Max. power consumption | 60 kVA (165 A) |
|  Transformer | 60 kVA |
|  Compression force (adjustable) | 1700 - 26000 kg |
|  Electrode dimensions | 140 x 140x60(h)mm |
|  Plate dimensions | 250 x 250x60(h)mm |
|  Aluminium frames dimensions | 168 x 148mm |
|  Max. mould height | 135mm |
|  Controller | PLC Siemens S5 |
|  Gas consumption | 5 – 20 l/min N2/Ar2 (max. 5% H2) |
|  Air consumption (filtered) | 2 l/min 6 bar |
|  Industrial water consumption | 40 - 50 l/min 2–6 bar |
|  Colour | Choice |
|  Overall size (approx.) | 1700x1700x2100(h) mm |
|  Weight (approx.) | 2000 kg |

* MGM reserve itself the right to change the characteristics described in this document without previous notice.