| *AUTOMATIC SINTERING MACHINE mod. IDRA 2T, WITH TWO STATIONS, 120 kVA, 42TON. |  |
| --- | --- |
| Main features |  |
|  Machine suitable for the continuous production of average/large series of diamond segments. |  |
|  The sintering process takes place in a controlled atmosphere in the 2 stations by inlet of inert/reducing gas. During the transport between the sintering to the cooling stations the mould is protected by a “shower” of the same gas. |  |
|  Temperature control with thermo-couple automatically inserted in the center of the mould. |  |
|  Type K thermo-couple for operating temperatures up to 1000°C. |  |
|  Evacuation system and smoke filtering with water filter. |  |
|  Sintering and cooling times are the same. |  |
|  Control program with cycles divided into 12 steps. Each step includes: |  |
|  temperature |  |
|  pressure |  |
|  max. power limit |  |
|  heating time |  |
|  holding time |  |
|  Memory allows for storing of up to 120 sintering programs. |  |
|  18 mould unloading and loading magazine. |  |
|  Automatic mould feeding from mould magazine. |  |
|  18 special aluminium frames. |  |
|  process data visualisation (set and real) and alarms. |  |
|  Machine complies with CE regulations. |  |
| #### Options |  |
|  Analogic outlet for variable process recording. |  |
|  Pyrometer 350-1300°C to be used alternatively to the thermo-couple. |  |
|  Height segment reading during sintering process (linear transducer on cylinder, resolution of 0.01 mm). |  |
|  Data acquisition system on external PC. |  |
|  Barcode reading system for automatic selection of sintering cycle according to product in aluminium frame, including labelling machine. |  |
|  36 moulds loading/unloading magazine. |  |
|  Aluminium frames. |  |
|  Thermo-couples. |  |
|  Electrodes in graphite. |  |
|  Graphite plates. |  |
|  Graphite moulds. |  |
|  Thermo-couples. |  |
|  Prearrangement for modem installation for remote assistance. |  |
| Technical Data |  |
|  Max. sintering area | 110 cm2 (850°C 350kg/cm2) |
|  Approx. sintering cycle time | 9 min. |
|  Productivity | 500-550 segm/h (40x2.8mm -90segm/mould) |
|  | 250-280 segm/h (24x10mm - 44segm/mould) |
|  Loading and unloading magazine | n.18 moulds |
|  Power supply | 380 / 400V 3phs 50Hz |
|  Max. power consumption | 120 kVA (175 A) |
|  Transformer | 120 kVA |
|  Compression force on the 2 stations (adjustable) | 3000 - 42000 kg |
|  Electrode dimensions | 150 x 160x60(h)mm |
|  Plate dimensions | 150 x 160x65(h)mm |
|  Aluminium frames dimensions | 193 x 158mm |
|  Max. mould height | 110mm |
|  Gas consumption | 15 – 25 l/min N2/Ar2 (max. 5% H2) |
|  Air consumption (filtered) | 10 l/min 6 bar |
|  Industrial water consumption | 80-100 l/min 2–6 bar 10-20°C |
|  Colour | Choice |
|  Overall size (approx.) | 2000x3250x2500(h) mm |
|  Weight (approx.) | 3500 kg |

* MGM  reserve itself the right to change the characteristics described in this document without previous notice.